DIRECT SHEAR EXERCISE

- In Lab

## Phase I

- Weight out ( 1.2 lb of dry Endcav and Millrock soils provided and measure area of shear chamber in in2.

- Disaggregate soil in mortar and pestle (do not crush grains).  Work under chemical hood.

- Add H20:	24% to Davidson

12% to Millrock

- Add H20 to soil and mix thoroughly.  Keep soil covered to prevent evaporation.

- Place one brass weight in bottom of shear chamber with fins at ( to stress direction.  Adjust the three spacing thumb screws in top ring to extend 1 mm.  Add top ring and secure with brass rods.

- Fill chamber to top with moist soil compacting gently with fingers.  Cap soil container to prevent evaporation.

- Compact to 50 inch pounds using torque wrench.  Add weight to soil to approximate 1 lb/in2.  (Weights of top brass plate and weight of assembly must be included).

- Back off the three spacing thumb screws and remove brass rods before shearing.

- Record meter reading.

- Apply stress at rate of one handle turn/1 second.

- Record maximum meter reading during shear (one unit on meter = 0.368 lb of force).

# Phase II

- Remove soil from chamber.  Note:  Use allen wrench to remove bottom half of shear chamber.

- Clean and replace shear chamber.

- Follow steps 5, 6 and 7 of Phase I again.

- Add weights to reach approximately 3 lb/in2.

- Back off the set screws and remove brass rods before shearing.

- Follow steps 9, 10, 11 of Phase I.

# Phase III

- Follow previous steps but add weight to approximately 6 lb/in2.

- Data Interpretation

# Construct a Mohrs Envelope

- Lay out X-Y axes with a scale of 1 unit of length = 1 pound per in2.

- Plot the 3 points resulting from (n and ( determined in lab.

- Construct a Mohr’s envelope.

- Using the envelope – plot a circle assuming a (n of 2 lb/in2.  Based on this circle report the following in lb/in2.

- (1

- (

- (n

- ( angle

- cohesion

- (

- Compare the two soils:

- Strength

- Source of strength

- Engineering applications